## Slide 1: Calculation of electronic structure and NMR parameters in organo-metallic materials
Gregor Mali, Andraž Krajnc, Jure Lapajne
Dirk De Vos, Bart Bueken, …

## Slide 2
NMR crystallography of paramagnetic catalysts
Measurement
  fast spinning
  variable temperature
  echo, low B0
Computation
  calculation of chemical and hyperfine shifts
  model systems, test computational approaches
Comparison
  assignment of measured and calculated signals
  causes of discrepancy

## Slide 3
nuclei are sensitive probes for local environment
they detect local magnetic field
isotropic shift depends on induced electric currents around a nucleus (chemical shift) and on spin density at the position of a nucleus (hyperfine coupling)

## Slide 4
nuclei are sensitive probes for local environment
+ + +
=
elektronska gostota na mestu jedra
chemical shift
hyperfine coupling
=

## Slide 5
DFT = density functional theory
pure dft: energy functional depends only on particle (electron) density n
hybrid dft: adds interactions between psi functions

## Slide 6
Quantum espresso:
  periodic lattice
  plane waves
  core electrons -> pseudopotential
Orca:
  single molecule or model structure
  all-electron calculation
CP2K:
  Mixture of above: plane waves + localized orbitals
Other well know packages:
  Q-chem, Nwchem, Gaussian, Castep, Abinit,...
Calculations of Aiso on model systems

## Slide 7
Model systems
Cu(acac)2 CuMOF-2 HKUST-1

## Slide 8
NMR in model systems: HKUST-1
1
2
3
228 ppm
853 ppm
-50 ppm
experimental | calculated
853 ppm | 802 ppm
228 ppm | 219 ppm
-50 ppm | -77 ppm

## Slide 9
1
2
3
NMR in model systems: Cu(acac)2
experimental | calculated
108 | 211
97 | 185
-53 | 79
Simple error checking:
diamagnetic acac
experimental | calculated
59 | 69
202 | 213
31 | 33
1
2
3
S=1/2
S=0

## Slide 10
Future work:
Compare planewave methods with all-electron methods
Test different energy functionals
Apply gained knowledge to test new molecules